# 13C CP MAS NMR spectra of laurate cellulose samples

# Experimental

13C CP MAS NMR spectra were recorded on Bruker AVANCE-II spectrometer at 14.1 T magnetic field using home built MAS probe for 25 x 4 mm Si3N4 rotors. In all experiments the spinning was 12.5 kHz. The NMR spectra were recorded with an ordinary Cross Polarization (CP) pulse sequence where the where the duration of ramped polarization transfer pulse was 1 ms, and the relaxation delay between the excitations was 5s. To get the right intensity distribution of the peaks for carbons in the long dynamic chains of fatty acids one should have record the spectra with direct excitation of carbons as well. Unfortunately, due to the long relaxation times of cellulose carbons the method of direct excitation needs too long experimental times.

Samples

Two cellulose laurate powder samples have been studied:

- Cel/Rex/Mini/Tj

- Fibrous/Cel/Rex/Mini/Tj.

Spectra

Figure 1. 13C CP MAS NMR spectrum of the sample 1 (Cel/Rex/Mini/Tj). The spectrum consists of the cellulose carbons resonances C1 to C6 and the peaks belonging to the lauric acid (C7 to C18). Despite of the fact that each resonance of the cellulose carbons is depending on the crystallinity of the sample, the integrals of the peaks, as given in the figure, show rather good correspondence to the number of sites. The degree of substitution DS can be evaluated as the ratio of the C7 integral to that of the C1 giving DS = 0.22. In the 13C CP MAS spectra of fatty acids, the intensities of the peaks belonging to the carbons of long dynamic chains are distorted. Here the 13C MAS spectrum obtained with direct excitation gives the right distribution of the peak intensities as given in the inset of the Figure.

Figure 2. 13C CP MAS NMR spectrum of the sample 2. The spectrum consists of the cellulose carbons resonances C1 to C6 and the peaks belonging to the lauric acid (C7 to C18). The degree of substitution DS, evaluated as the ratio of the C7 integral to that of the C1 gives DS = 0.15, much smaller than for the sample 1. The inset shows the 13C MAS spectrum obtained with direct excitation, which gives the right distribution of the peak intensities in fatty acids.